N 1706 DINACOMB EVOLUTION

|  | (*) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | T °C | 260 |  |
|  | p bar |  | 500 | 25 |  |
|  | V m/s |  | 3.5 | 15 |  |
|  | pH | 1 ( 13 |  |

(*) Do not use the product to the maximum temperature and pressure associated without consulting the manufacturer

| Composition |  | size mm size inch kg/box lbs/box mt/box ft/box mt/kg ft/lbs 3,0 1/8 1,0 2,2 79,4 260 79,4 118,2 4,0 - 1,0 2,2 44,6 146 44,6 66,5 5,0 3/16 1,0 2,2 28,6 94 28,6 42,6 6,0 - 2,5 5,5 49,6 163 19,8 29,6 6,5 1/4 2,5 5,5 42,3 139 16,9 25,2 8,0 5/16 2,5 5,5 27,9 92 11,2 16,6 9,5 3/8 2,5 5,5 19,8 65 7,9 11,8 10,0 - 2,5 5,5 17,9 59 7,1 10,6 11,0 7/16 2,5 5,5 14,8 48 5,9 8,8 12,0 - 2,5 5,5 12,4 41 5,0 7,4 12,7 1/2 2,5 5,5 11,1 36 4,4 6,6 14,0 9/16 5,0 11,0 18,2 60 3,6 5,4 16,0 5/8 5,0 11,0 14,0 46 2,8 4,2 17,5 11/16 5,0 11,0 11,7 38 2,3 3,5 18,0 - 5,0 11,0 11,0 36 2,2 3,3 19,0 3/4 5,0 11,0 9,9 32 2,0 2,9 22,0 7/8 5,0 11,0 7,4 24 1,5 2,2 25,5 1 5,0 11,0 5,5 18 1,1 1,6 Packaged +/- 10 % in weight |
| --- | --- | --- |
| - special organic yarn - impregnation with PTFE - solid lubricant |  |  |
| Features |  |  |
| N1706 Dinacomb is a special packing braided with a new generation high tenacity yarn, with chemical and mechanical properties better than the PPTA yarn. N1706 Dinacomb offers both a better performance with the most frequent chemical fluids, where the PPTA is not suitable, and big resistance in the abrasive applications. In order to improve the sliding properties Dinacomb is impregnated with a special solid lubricant. |  |  |
| Applications |  |  |
| Dinacomb evolutions is suitable in all dynamic application in the range 1÷13. |  |  |